## Slide 1
Charge Carrier Dynamics in Hybrid Perovskites:
Insights from NAMD Simulations
Dibyajyoti Ghosh
Los Alamos National Laboratory
LA-UR-20-21858

## Slide 2
Methylammonium lead iodide CH3NH3PbI3
Organic-Inorganic Perovskite
Kojima et al. J. Am. Chem. Soc, 2009, 131, 6050
Eames et. al. Nature Comm. 2015, 6, 7497
Lin et al. Science, 2020, 369, 6499
Solution processable
Strong absorption
Excellent charge transport
Defect tolerant
Tunable Dimensionality
Layered Perovskites (2D)
Tsai et al. Nature, 2016, 536, 7616
Shi et al. Nature, 2020, 580, 614
Quantum Dots (0D)
Raino et al. Nature, 2018, 563, 671
Swarnkar et al. Angew. Chem., 2015, 127, 15644
A cations
B metals: Pb, Sn

## Slide 3: 2D-halide perovskites
Grancini et al. Nat. Rev. Mater., 2019, 4, 4;
Smith et al. Chem. Rev, 2019, 119, 3104
Wide diversity in crystal structure and emission properties
Conceptual slicing of a 3D-perovskite
Improved stability
Higher crystallinity and fewer defects
Promising light absorption and emission

## Slide 4: Two-dimensional perovskites for Optoelectronics
Tsai et al. Nature 2016, 536, 312; Blancon et al. Science 2017, 355, 1288; Tsai et. al, Science Advances 2020, 6, 0815
Partially known complex nature of carrier recombination dynamics
B = Pb, Sn
X = Cl, Br, I
What is the role of spacer cations on the carrier recombination processes ?

## Slide 5: Different Spacer Cations in 2D perovskites
Similar crystal structure and static electronic properties
BA
(Alkyl chain)
PEA
(Benzene ring)
Well studied and distinctly different optoelectronic (LED, detectors) performances
BA+
PEA+
BA+
PEA+
Takagi et al. Phys. Rev. B, 2013, 87, 125421
Gong et al. Nature Mater, 2018, 17, 550

## Slide 6: Key Questions
How spacer cations impact the electronics?
Influences in structural dynamics?
What about non-radiative recombination rates?
Methods
Density functional theory &
ab initio molecular dynamics
Non-adiabatic molecular dynamics
t
E
j
i
Static Structure and Properties with DFT
Structural Fluctuations with AIMD

## Slide 7: Computational Approach
AIMD (with VASP)
Step 1: Optimize the structure at 0 K
Step 2: Gradually heat the lattice to 300 K
Step 3: Keep the lattice at 300 K and generate the trajectory (NVE ensemble)
Calculate non-adiabatic coupling constants (with VASP)
Step 1: Separate the trajectory in smaller fragments
Step 2: Calculate adiabatic state energies and NA coupling between states
NAMD simulation (with PYXAID)
Calculate the change of state populations over time. Used classical path approximation and decoherence induced surface hopping (DISH).

## Slide 8: Static Electronic Properties
(BA)2PbBr4
(PEA)2PbBr4
VBM
CBM
VBM
CBM
3.13 eV
3.14 eV
Similar band gaps
Molecular states are well below (>1eV) to band-edges
PEA states are relatively closer to VBM
Ghosh et al. J. Phys. Chem. Lett, 2020, 11, 2955
DFT, 0 K

## Slide 9
Impact of Spacer Cations on Carrier Dynamics
Population of electron-hole recombined state through non-radiative processes (dominant loss mechanism)
Ghosh et al. J. Phys. Chem. Lett, 2020, 11, 2955;
Ghosh et al. J. Mater. Chem. A, Just Accepted, 2020
Much faster non-radiative recombination for (BA)2PbBr4
(BA)2PbBr4
(PEA)2PbBr4
Recombined carrier

## Slide 10: Spacer Cation Dependent Structural Dynamics
BA cations make PbBr-layer more dynamic
(PEA)2PbBr4 is more rigid;  stacking interactions
AIMD, 300 K
Ghosh et al. J. Phys. Chem. Lett, 2020, 11, 2955

## Slide 11: Dynamic Electronic Properties
Band gaps and excited states fluctuate more for BA-based perovskites
Strong influence of dynamic structures on the electronic properties
VBM
CBM

## Slide 12: Non-adiabatic Coupling
More number of large NAC values for (BA)2PbBr4
Dynamic (BA)2PbBr4: Stronger electron-phonon interactions, more active non-radiative processes

## Slide 13: Next Step: In silico materials designing for efficient 2D Iodide perovskites
3AMP2+
(A)PbI4
Ghosh et al. Accepted, J. Mater. Chem. A 2020
Two spacer cations/unit;
Non-covalent stacking
3AMP (Stiffest)
BA
(Most dynamic)
BA+
PEA+
(A)2PbI4
Single spacer cation/unit;
stiff stacking
Design Strategy for 2D halide perovskites:
Compact the interlayers, mitigated fluctuations; slower the non-radiative recombination

## Slide 14: 2D-halide Perovskites for Optoelectronics
Dynamic structures influence the charge carrier recombination processes: Strategic structural modifications can mitigate non-radiative losses

## Slide 15
Group & Collaboration
Dr. Sergei Tretiak and Dr. Amanda Neukirch (LANL)
Prof. Oleg Prezhdo (USC)and group
Dr. W. Nei (LANL)