## Slide 1: Photoexcitation Dynamics in Perylene Diimides
Aliya Mukazhanova
DMR-1847774

## Slide 2: Perylene Diimide
Promising for organic optoelectronics and light harvesting
Controllable electronic characteristics
Outstanding chemical, thermal and photostability
High electron conductivity, strong light absorption
Affinity to self-assemble
Perylene-3,4,9,10-tetracarboxylic diimide
(PTCDI)
https://phys.org/news/2015-06-optimized-enables-custom-electronics.html
https://scitechdaily.com/new-flexible-ultrathin-organic-solar-cell-is-both-highly-efficient-and-durable/

## Slide 3: Perylene Diimide
Transport optical excitation energy efficiently1-3
The excited-state lifetime and decay pathway are highly dependent on inter-molecular orientation4-7
This work: How inter-molecular interactions influence energy transfer and exciton localization dynamics? What vibrational modes assist the electronic relaxation?
1. Mazaheripour, A. et al. Mater. Horizons 2017, 4 (3), 437–441
2. Schubert, A. Et al. J. Phys. Chem. A 2014, 118 (8), 1403–1412
3. Ma, L. et al. J. Phys. Chem. A 2014, 118 (5), 838–843 (11)
4. Brown, K. E. et al. J. Phys. Chem. Lett. 2014, 5 (15), 2588–2593.
5. Farag, M. H. et al. J. Phys. Chem. C 2018, 122 (45), 25753–25763.
6. Le, A. et al. J. Am. Chem. Soc. 2018, 140 (2), 814–826.
7. Wirsing, S. et al.J. Phys. Chem. C 2019.
https://phys.org/news/2015-06-optimized-enables-custom-electronics.html
https://scitechdaily.com/new-flexible-ultrathin-organic-solar-cell-is-both-highly-efficient-and-durable/
monomer
dimer
trimer

## Slide 4: Non-adiabatic Excited State Dynamics
R
S0
S2
S1
∆
T. Nelson, S. Fernandez-alberti, V. Chernyak, A. E. Roitberg and S. Tretiak J. Phys. Chem. B, 2011, 115, 5402; T. Nelson, S. Fernandez-Alberti, A. E. Roitberg and S. Tretiak Acc. Chem. Res., 2014, 47, 1155; J. C. Tully J. Chem Phys., 1990, 93, 1061.
Classical molecular dynamics
run for 300 ps
AM1 Hamiltonian
700 trajectories
Tully’s fewest switches surface hopping 1 ps trajectory
(t) + A(t)
Langevin equation of motion for nuclei
Time-dependent expansion coefficients
ℏ=
With Sergei Tretiak (LANL)
Sebastian Fernandez-Alberti (The National University of Quilmes)
Ground state wavepacket
Excited-State Spectrum
Non-adiabatic excited state dynamics
Ground state geometry
Optimized with wB97-XD functional in Gaussian16 code

## Slide 5: Monomer Internal Conversion Dynamics
Excite S2, non-radiative decay to S1 over ~ 1 ps
A. Mukazhanova, W. Malone, H. Negrin-Yuvero, S. Fernandez-Alberti, S. Tretiak, S. Sharifzadeh, JCP (2020)
50% decay to S1 at 860 fs

## Slide 6: Vibrational Excitations from Franck-Condon analysis : monomer
Mode 113
Mode 101
Mode 102
Franck-Condon spectrum
H. Negrin Yuvero, A. Mukazhanova, V. Freixas, S. Tretiak, S. Sharifzadeh, S. Fernandez-Alberti, J. Phys. Chem. A (2022)
Atomic motion suggests Franck-Condon active C-C breathing modes important for dynamics
Notes: Notes:
Figure (top): Representation of the different 𝒅_1,2^(𝑆𝑉𝐷,𝑖) associated with the vibronic couplings for monomer PTCDI non-adiabatic dynamics. The vertical dashed line separates the molecules in the two segments that have the same vibronic dynamics.SVD has been performed on the non-adiabatic derivative coupling between S1 and S2, 𝒅_12, collected from the different NEXMD simulations at the moment of effective S2S1 transitions to obtain the associated representative atomic motions.
Figure (middle): dominant modes from dynamics
Figure (bottom): FC analysis. The first peak (set to 0 cm-1 ) contain mainly 00 transition. The second peak at ~1700 cm-1 has contributions from 01 transition of modes 101, 102, 113 for a-PDI. These modes 101, 102 for a-PDI are degenerate and not present during photoexcitation dynamics. Vibrational mode 113 actively participate in energy transfer during dynamics.

## Slide 7: Vibrational Excitations During Dynamics: monomer
Mode 113
Mode 101
Mode 102
Franck-Condon active modes
Two different vectors of non-adiabatic derivative couplings d12 are identified using the singular value decomposition (SVD)
Mode 112
Mode 113
Modes #112 and #113 provide dominant contributions to and
Hassiel Negrin-Yuvero
Victor Frexias
H. Negrin Yuvero, A. Mukazhanova, V. Freixas, S. Tretiak, S. Sharifzadeh, S. Fernandez-Alberti, J. Phys. Chem. A (2022)
Notes: Notes:
Figure (top): Representation of the different 𝒅_1,2^(𝑆𝑉𝐷,𝑖) associated with the vibronic couplings for monomer PTCDI non-adiabatic dynamics. The vertical dashed line separates the molecules in the two segments that have the same vibronic dynamics.SVD has been performed on the non-adiabatic derivative coupling between S1 and S2, 𝒅_12, collected from the different NEXMD simulations at the moment of effective S2S1 transitions to obtain the associated representative atomic motions.
Figure (middle): dominant modes from dynamics
Figure (bottom): FC analysis. The first peak (set to 0 cm-1 ) contain mainly 00 transition. The second peak at ~1700 cm-1 has contributions from 01 transition of modes 101, 102, 113 for a-PDI. These modes 101, 102 for a-PDI are degenerate and not present during photoexcitation dynamics. Vibrational mode 113 actively participate in energy transfer during dynamics.

## Slide 8: Stacking Leads to Faster Dynamics
Excited at S4
50% decay to S1 at 400 fs
Excited at S2
50% decay at > 1 ps
Excited at S6
50% decay to S1 at 240 fs
A. Mukazhanova, H. Negrin-Yuvero, V. Frexias, S. Fernandez-Alberti, S. Tretiak, S. Sharifzadeh, J. Mater. Chem. C (2023)
S1
S2
0.52
S1
S2
S3
S4
0.20
0.37
0.64
0.69
S1
S2
S3
S4
S5
S6
0.12
0.1
0.38
Reduced energy splitting results in more efficient funneling of energy

## Slide 9: Stacking Leads to Faster Dynamics
The analysis of non-adiabatic coupling terms (NACT) explains increase of energy decay in stacked molecules
The internal energy conversion has a sequential character from highest to lower excited state
A. Mukazhanova, H. Negrin-Yuvero, V. Frexias, S. Fernandez-Alberti, S. Tretiak, S. Sharifzadeh, J. Mater. Chem. C (2023)

## Slide 10: Vibrational Excitations During Dynamics: dimer
Effective hop |  | Effective hop | 
S3→S2 |  | S2→S1 | 
# Mode | Overlap | # Mode | Overlap
226(1865) | 0.78 | 226(1865) | 0.88
209(1693) | 0.27 | 223(1795) | 0.16
207(1679) | 0.25 | 222(1792) | 0.16
222(1792) | 0.14 | 207(1679) | 0.14
199(1596) | 0.13 | 225(1797) | 0.12
223(1795) | 0.13 | 122(908) | 0.10
122(908) | 0.11 | 121(904) | 0.10
175(1416) | 0.10 | 209(1693) | 0.10
121(904) | 0.10 | 224(1795) | 0.09
234(2025) | 0.09 | 234(2025) | 0.08
Similar vibrational modes assists the energy transfer making it more efficient and faster
Hassiel Negrin-Yuvero
Victor Frexias
A. Mukazhanova, H. Negrin-Yuvero, V. Frexias, S. Fernandez-Alberti, S. Tretiak, S. Sharifzadeh, J. Mater. Chem. C (2023)
Notes: Notes:
Figure (top): Representation of the different 𝒅_1,2^(𝑆𝑉𝐷,𝑖) associated with the vibronic couplings for monomer PTCDI non-adiabatic dynamics. The vertical dashed line separates the molecules in the two segments that have the same vibronic dynamics.SVD has been performed on the non-adiabatic derivative coupling between S1 and S2, 𝒅_12, collected from the different NEXMD simulations at the moment of effective S2S1 transitions to obtain the associated representative atomic motions.
Figure (middle): dominant modes from dynamics
Figure (bottom): FC analysis. The first peak (set to 0 cm-1 ) contain mainly 00 transition. The second peak at ~1700 cm-1 has contributions from 01 transition of modes 101, 102, 113 for a-PDI. These modes 101, 102 for a-PDI are degenerate and not present during photoexcitation dynamics. Vibrational mode 113 actively participate in energy transfer during dynamics.

## Slide 11: Vibrational Excitations During Dynamics: trimer
Activated vibrational modes are different from dimer case
Mode # 256
Mode # 257
Mode # 258
Mode # 259
Mode # 262
Mode # 265
Mode # 316
Mode # 325
Effective hops |  |  |  |  | 
S4→S3 |  | S3→S2 |  | S2→S1 | 
# Mode | Overlap | # Mode | Overlap | # Mode | Overlap
259 (1410) | 0.45 | 256 (1402) | 0.51 | 256 (1402) | 0.53
325 (1763) | 0.38 | 265 (1431) | 0.40 | 265 (1431) | 0.39
257 (1408) | 0.37 | 316 (1719) | 0.37 | 316 (1719) | 0.38
265 (1432) | 0.32 | 259 (1410) | 0.33 | 258 (1408) | 0.31
262 (1419) | 0.25 | 258 (1408) | 0.31 | 259 (1410) | 0.31
264 (1428) | 0.16 | 310 (1647) | 0.18 | 310 (1647) | 0.18
261 (1418) | 0.16 | 274 (1480) | 0.18 | 274 (1480) | 0.17
294 (1580) | 0.15 | 261 (1418) | 0.12 | 271 (1476) | 0.11
286 (1524) | 0.14 | 271 (1476) | 0.11 | 261 (1418) | 0.10
244 (1335) | 0.13 | 287 (1525) | 0.09 | 264 (1428) | 0.10
A. Mukazhanova, H. Negrin-Yuvero, V. Frexias, S. Fernandez-Alberti, S. Tretiak, S. Sharifzadeh, J. Mater. Chem. C (2023)
Notes: Notes:
Figure (top): Representation of the different 𝒅_1,2^(𝑆𝑉𝐷,𝑖) associated with the vibronic couplings for monomer PTCDI non-adiabatic dynamics. The vertical dashed line separates the molecules in the two segments that have the same vibronic dynamics.SVD has been performed on the non-adiabatic derivative coupling between S1 and S2, 𝒅_12, collected from the different NEXMD simulations at the moment of effective S2S1 transitions to obtain the associated representative atomic motions.
Figure (middle): dominant modes from dynamics
Figure (bottom): FC analysis. The first peak (set to 0 cm-1 ) contain mainly 00 transition. The second peak at ~1700 cm-1 has contributions from 01 transition of modes 101, 102, 113 for a-PDI. These modes 101, 102 for a-PDI are degenerate and not present during photoexcitation dynamics. Vibrational mode 113 actively participate in energy transfer during dynamics.

## Slide 12: Backbone Slows Internal Energy Conversion Dynamics
Rapid transfers (within a few fs) from higher energy states to S3 and a slower decay from S3 to S1.
There is 50% population transfer from S3 to S1 at 400fs for dimer and at 1500fs for dimer with backbone.
Why backbone slows down the dynamics?
A. Mukazhanova, H. Negrin-Yuvero, V. Frexias, S. Fernandez-Alberti, S. Tretiak, S. Sharifzadeh, J. Mater. Chem. C (2023)

## Slide 13: Exciton Localization in Dimer
Example trajectory:
After decay to S1, excited-state localizes and hops between molecules

## Slide 14: Exciton Delocalization in Trimer
After decay to S1 (246 fs), excited-state delocalizes

## Slide 15: Conclusions
Photo-induced excited-state dynamics of functionalized perylene diimide monomer, dimer and trimer
The stacking accelerates the energy transfer due to reduced effective energy gap and activation of similar vibrational modes
The set of activated vibrational modes are different in dimer than in trimer.
The backbone slows down the relaxation rate
The Sharifzadeh group
Collaborators:
Walter Malone (LANL)
Hassiel Negrin-Yuvero (UNQ)
Victor Frexias (UNQ)
Sebastian Fernandez-Alberti (UNQ)
Sergei Tretiak (LANL)
Funding
DMR-1847774