## Slide 1: Fragment orbital-based surface hopping (FOB-SH): Method, Implementation, Application
Vista Seminar Series
22.10.2020
Jochen Blumberger
University College London
Department of Physics and Astronomy

## Slide 2: Content
FOB-SH: a tool for simulating electronic transport processes in truly nanoscale molecular materials
Application to charge transport in
organic crystals and the emergence
of large ``flickering” polarons
Tricks of the Trade: importance of decoherence correction, trivial crossing detection and all that

## Slide 3
Workhorse for photochemistry
But: ad-hoc/intuitive, no nuclear tunneling,….
Crespo-Otero and Barbatti
Chem. Rev. 118, 7026 (2018)
(Tully, J. Chem. Phys. 1990)

## Slide 4
Challenge 1: Ascending (another) Jacob’s ladder
.
.
.
Multiconfigurational time-dependent Hartree (Meyer,…)
(Classical limit of) Exact factorisation of molecular wavefunction (Gross,…)
Ab-initio multiple spawning (Martinez,…)
Ring-polymer MD with non-adiabatic transitions (T. Miller,…)
Fewest switches surface hopping (Tully,…)
Ehrenfest dynamics (Ehrenfest)

## Slide 5: Challenge 2 (this talk): Going bigger
Non-adiabatic dynamics at the true nanoscale (> 5 nm):
Exciton dissociation
to charges, recombination
Energy transfer
Solar Cells
Organic
Transistors
Charge transport
Light
harvesting
Electronic processes can be strongly delocalized in space (no QM/MM)
and non-periodic (no periodic supercells)
+

## Slide 6: Molecular  True Nanoscale: How?
10 femtosecond/day
100 atoms
1 picoseconds/day
100,000 atoms
TDDFT
SH
??

## Slide 7: Molecular  True Nanoscale
10 femtosecond/day
100 atoms
1 picoseconds/day
100,000 atoms
TDDFT
SH
Fragment Orbital-Based
Surface Hopping
Fragment and
Conquer
J. Spencer, F. Gajdos, JB, JCP 145, 064102, 2016.
A. Carof, S. Giannini, JB, JCP 147, 214113, 2017.
S. Giannini, A. Carof, JB JPCL, 9, 3116, 2018.
A. Carof et al. PCCP 21, 26368, 2019.
S. Giannini et al. Nat. Comm. 10, 3843, 2019.
S. Giannini et al. Adv. Theor. Simul. 3, 2000093, 2020.
FOB
SH
Martinez, Burghardt,
Akimov, Elstner,.....

## Slide 8: FOB-SH implemented for:
Charge transport in molecular materials (this talk)
Exciton transport in molecular materials (upcoming VISTA talk by Samuele Giannini(?))
Exciton dissociation and charge recombination at nanoscale materials interfaces (in progress)

## Slide 9
Charge transport in molecular materials
DFT band structure
 narrow bands
rubrene

## Slide 10
Charge transport in molecular materials
Valence Band (VB)
DFT band structure
VB ≃ linear combinations
of HOMOs
 narrow bands
rubrene

## Slide 11
Charge transport in molecular materials
Valence Band (VB)
DFT band structure
+
Hole Transport
in VB
VB ≃ linear combinations
of HOMOs
 narrow bands
rubrene
kBT
Non-adiabatic dynamics
of hole in valence band

## Slide 12: FOB-SH for charge transport
Hole wavefunction:
Schrodinger equation for hole:
Classical nuclear dynamics
Stochastic hopping from
surface Ei  Ej with
probability
electron hole
nuclei
ith adiabatic electronic state
ϕ1
ϕ2
ϕ3
state
1
2
3
.
.
State basis of HOMO orbitals
JCP 145, 064102 (2016), JCP 147, 214113 (2017), JPCL 9, 3116 (2018), PCCP 21, 26368 (2019)
Antoine Carof

## Slide 13: 1. Fast calculation of Hole Hamiltonian
I
I
I
I
I
I
I
I
1
4
7
2
5
3
6
9
I
8
H =
ϕ1
ϕ2
ϕ3
force field
Analytic overlap
method (AOM)
Hole Hamiltonian (``Tight binding”):
J. Spencer, F. Gajdos, JB, JCP 145, 064102, 2016.

## Slide 14
Ultrafast estimation of electronic couplings
F. Gajdos, JB et al. J. Chem. Theor. Comput. 10, 4653 (2014).
blue symbols
=
Training set
(black line)
other symbols
=
Test sets
mean error = factor 1.9
over 5 decades!

## Slide 15: Speed-up of 6 orders of magnitude, 20% loss of accuracy
F. Gajdos, JB et al. J. Chem. Theor. Comput. 10, 4653 (2014).

## Slide 16: Density of states rubrene valence band
top of
valence band
Good agreement AOM vs sDFT for peak position
and band width (0.5 eV)

## Slide 17: 2. Fast calculation of nuclear gradients
J. Spencer, F. Gajdos, JB, JCP 145, 064102, 2016
A. Carof, S. Giannini, JB, JCP 147, 214113, 2017
nuclear force on
adiabatic PES i
off-diagonal gradients in HOMO basis
(diagonal gradient from force field)
NACV in HOMO basis
(finite difference)
overlap gradients in HOMO basis
Antoine Carof
NACV between PESs i,j

## Slide 18: 3. Making surface hopping work
Decoherence correction: damping of inactive states
using frozen Gaussian approximation
Detection of trivial crossing: (i) State tracking algorithm
(ii) Enforcing sum rule:
Removal of decoherence-correction induced artificial long-range CT
via projection of wavefunction in moving active region
Schwartz, Bittner, Prezhdo, Rossky,
JCP 104, 5942 (1996)
Wang and Prezhdo,
JPCL 5, 713 (2014)
Giannini, Carof, JB
JPCL (2018)
Giannini, Carof, JB JPCL (2018)
similar to Tretiak’s algorithm

## Slide 19: Content
FOB-SH: a tool for simulating electronic transport processes in truly nanoscale molecular materials
Application to charge transport in organic crystals
and the emergence of large ``flickering” polarons
Tricks of the Trade: importance of decoherence correction, trivial crossing detection and all that

## Slide 20: Organic Single Crystals
Samuele Giannini

## Slide 21: Hole transport in conductive plane at 300K
Giannini et al. Nature Comm. 10, 3843, 2019; Adv. Theor. Simul. 3, 2000093, 2020.
pMSB
small polaron hopping
< 1
A

## Slide 22: Hole transport in conductive plane at 300K
Giannini et al. Nature Comm. 10, 3843, 2019; Adv. Theor. Simul. 3, 2000093, 2020.
pMSB
rubrene
small polaron hopping
large (``flickering”) polaron
> 1
< 1
A

## Slide 23: Transport Mechanism from FOB-SH
AAAA
AAAA
AAAA
AAAA
energy (meV)
0
50
100
150
IPR = inverse participation ratio
(number of molecules over which
charge is delocalized)
a index = active state PES in FOB-SH
AAAA
AAAA
AAAA
AAAA
Giannini et al. Adv. Theor. Simul. 3, 2000093, 2020.

## Slide 24: Transport Mechanism from FOB-SH
AAAA
AAAA
AAAA
AAAA
energy (meV)
0
50
100
150
IPR = inverse participation ratio
(number of molecules over which
charge is delocalized)
a index = active state PES in FOB-SH
AAAA
AAAA
AAAA
AAAA
Giannini et al. Adv. Theor. Simul. 3, 2000093, 2020.

## Slide 25: Transport Mechanism from FOB-SH
AAAA
AAAA
AAAA
AAAA
energy (meV)
0
50
100
150
IPR = inverse participation ratio
(number of molecules over which
charge is delocalized)
a index = active state PES in FOB-SH
AAAA
AAAA
AAAA
AAAA
Giannini et al. Adv. Theor. Simul. 3, 2000093, 2020.

## Slide 26: Transport Mechanism from FOB-SH
AAAA
AAAA
AAAA
AAAA
energy (meV)
0
50
100
150
IPR = inverse participation ratio
(number of molecules over which
charge is delocalized)
a index = active state PES in FOB-SH
Giannini et al. Adv. Theor. Simul. 3, 2000093, 2020.

## Slide 27
From trajectories to charge mobilities
Mean-Square Displacement
Diffusion coefficient
Charge mobility
MSD(t)
slope
1000 traj

## Slide 28
Charge mobility: FOB-SH vs Experiment
small
polaron
medium
polaron
large
polaron
Giannini et al. Nature Comm. 10, 3843, 2019; Adv. Theor. Simul. 3, 2000093, 2020.

## Slide 29
What limits charge mobility in organic crystals?
Thermal fluctuations of electronic coupling
A
couplings frozen
to mean value
couplings fluctuate
(as before)
Giannini et al. Nature Comm. 10, 3843, 2019.

## Slide 30: Content
FOB-SH: a tool for simulating electronic transport processes in truly nanoscale molecular materials
Application to charge transport in organic crystals
and the emergence of large ``flickering” polarons
Tricks of the Trade: importance of decoherence correction, trivial crossing detection and all that

## Slide 31: 1. Energy criterion for hops: Kinetic energy || NACV  Detailed balance
2 Hab
P1surf, full kinetic energy
P1B, exact Boltzmann weight
P1surf, kinetic energy || NACV
no frustrated
hops
P1B
P1surf = population of excited
state PES in FOB-SH
Detailed balance:
P1surf = P1B
JCP 147, 214113 (2017)

## Slide 32: 2a Decoherence correction  Internal consistency
PiB
Pisurf = population of adiabatic PES i
in FOB-SH
Piwf = population of electronic adiabatic
wavefunction i in FOB-SH
Internal consistency
Pisurf = Piwf
Giannini et al. Nature Comm. 10, 3843, 2019.

## Slide 33: 2b Decoherence correction  convergence of mobility
 Mobilities diverge with system size without decoherence
PCCP 21, 26368 (2019)

## Slide 34: 3. Spurious charge transfer correction (SCTC)  physical CT dynamics
AAAA
AAAAAA
AAAA
AAAA
AAAA

## Slide 35: 4. Detection of trivial crossings  physical CT dynamics
PCCP 21, 26368 (2019)

## Slide 36: Summary
Developed a non-adiabatic MD method for real-time propagation of
charge carriers in ``soft” materials
Practical: -large systems (1000 sites ≙105 valence electrons)
-convergence: 103 trjs 1ps each in 1 day on 103 cores
Predictive: Experimental mobilities well reproduced
New picture of charge carriers in ``soft” materials: not hopping, not band
Provides numerical benchmarks for new theories
e.g. transient localization theory, stochastic Liouville
Useful: Prediction of charge mobility in new materials

## Slide 37: Outlook
Extending state space of electronic Hamiltonian in FOB-SH
Exciton transport (VISTA talk by Samuele Giannini (?))
Charge separation and recombination at n-p type interfaces (excitonic solar cells)
Exciton dissociation at n-p type interfaces
Beyond Surface Hopping
 Classical limit of exact factorisation (Abedi, Gross, Agostini,…)
Ehrenfest + quantum momentum terms
Problem: Divergence of quantum momentum in Eq. S28 of Min et al. JPCL 2017
Surface Hopping with Quantum Nuclei/RPMD (Tully, Shushkov, Miller,…)
Problem: Many beads but only one electronic SE. Expensive.

## Slide 38
Acknowledgements
Antoine Carof
Samuele Giannini
Matt Ellis
Soumya Ghosh

## Slide 39
Acknowledgements
Orestis Ziogos
Wei-Tao Peng
Jan Elsner

## Slide 40
23-25 June 2021
Face-to-face,
Virtual or
Hybrid

## Slide 42: Fragment orbital-based surface hopping (FOB-SH)
2 major approximations:
1. Exact electron-nuclear quantum dynamics replaced by
mixed quantum-classical dynamics
2. Time-dependent multi-determinantal electronic wavefunction replaced by
a 1-particle wavefunction describing the excess electron or hole
NO explicit core and valence electrons.
Implicitly included by parametrization of electronic Hamiltonian.

## Slide 43
Analytic Overlap Method (AOM) for electronic couplings Hkl (as published)

## Slide 44: Density of states and IPR (new data)

## Slide 45: Detailed balance and internal consistency
Rescale velocities || NACV  detailed balance
Decoherence correction  internal consistency

## Slide 46
Summary: Nature of holes in OS crystals
Giannini et al. Nature Comm. 10, 3843, 2019.

## Slide 47
Summary: Nature of holes in OS crystals
Giannini et al. Nature Comm. 10, 3843, 2019.

## Slide 48: Convergence IPR wrt system size (new data)
(polaron size)
(system size)

## Slide 49: Convergence 2D mobility wrt system size

## Slide 50: Convergence IPR wrt time step (new data)
(polaron size)

## Slide 51: Convergence 2D mobility wrt time step (new data)

## Slide 52
Mobility correlates well with polaron size (as published)
Giannini et al. Nature Comm. 10, 3843, 2019.