## Slide 1
Enhancing Interlayer Charge Transport of Two-Dimensional Perovskites by Structural Stabilization via Fluorine Substitution
Liz Stippell
PhD Candidate: University of Southern California
Advisor: Prof. Oleg Prezhdo

## Slide 2: The Search for Better Energy Materials: Two-Dimensional Perovskites
Question:
How can we improve the efficiency of 2D perovskites?
Answer:
Adjust the organic spacers to enhance charge transfer
Wu, G. et al. Advanced Materials 2022, 34 (8), 2105635.
Notes: Sources:
https://www.researchgate.net/figure/Schematic-illustration-for-2D-perovskites-3D-perovskites-and-mixed-dimensional_fig1_356789331

## Slide 3: Using Fluorine to Enhance Charge Transfer
Benzylammonium (BZA)
F
Fluorinated-Benzylammonium (F-BZA)
Why the para- position?
Yan, G. Chemistry of Materials 2022, 34 (7), 3346-3356.
Wang, Z. ACS Applied Materials & Interfaces 2022, 14 (6), 7917-7925.
PCE
Question:
HOW does fluorine improve charge transfer and efficiencies?
Notes: Sources: SHOW EXPERIMENTAL WORK
PARA VS OTHER POSITIONS
https://www.researchgate.net/figure/Schematic-illustration-for-2D-perovskites-3D-perovskites-and-mixed-dimensional_fig1_356789331

## Slide 4: Understanding Charge Transfer: Marcus Theory
Marcus rate coupling ()
Marcus rate site energies-1
Charge Carrier Hopping Mobility
Marcus, R. A. The Journal of Chemical Physics 1965, 43 (8), 2654-2657.
Notes: Sources:
https://www.researchgate.net/figure/Schematic-illustration-for-2D-perovskites-3D-perovskites-and-mixed-dimensional_fig1_356789331

## Slide 5: Projection Diabatization Method (POD): Computing Nonadiabatic Couplings
Fragment-based diabatization method
Create donor and acceptor blocks
Diagonalize each block separately
Donor
Acceptor
Donor Energies
Acceptor Energies
Donor-Acceptor Couplings
Kondov, I. The Journal of Physical Chemistry C 2007, 111 (32), 11970-11981.
Notes: Sources:
https://www.researchgate.net/figure/Schematic-illustration-for-2D-perovskites-3D-perovskites-and-mixed-dimensional_fig1_356789331

## Slide 6: Fluorine’s Effects on Electronic Structure
Charge density migrates to fluorine
Potential to enhance charge transfer
Fluorine does NOT contribute to band edge states
Fluorine has minimal influence in coupling
HOMO
LUMO
Non-Fluorinated
Fluorinated
Notes: Sources:
https://www.researchgate.net/figure/Schematic-illustration-for-2D-perovskites-3D-perovskites-and-mixed-dimensional_fig1_356789331

## Slide 7: Fluorine’s Effects on Marcus Rate: Nonadiabatic Coupling & Reorganization Energy
HOMO ~ -2.5 eV
HOMO ~ -2.75
Non-Fluorinated
Fluorinated
POD Method
Notes: Sources:
https://www.researchgate.net/figure/Schematic-illustration-for-2D-perovskites-3D-perovskites-and-mixed-dimensional_fig1_356789331

## Slide 8: Putting the pieces together: charge transfer rates
 |  | (meV) | (eV) |  | L (Å) | (cm2 V-1 s-1)
Non-Fluorinated | LUMO | 0.442 | 0.907 | 1.790 s | 14.073 | 4.255*10-7
 | HOMO | 4.261 | 0.632 | 1.142 ns |  | 6.668*10-4
Fluorinated | LUMO | 0.435 | 0.547 | 44.812 ns | 13.482 | 1.560*10-5
 | HOMO | 3.663 | 0.498 | 0.377 ns |  | 1.852*10-3
 |  |  |  |  | L (Å) | 
Non-Fluorinated | LUMO | 0.442 | 0.907 |  | 14.073 | 4.255*10-7
 | HOMO | 4.261 | 0.632 | 1.142 ns |  | 6.668*10-4
Fluorinated | LUMO | 0.435 | 0.547 | 44.812 ns | 13.482 | 1.560*10-5
 | HOMO | 3.663 | 0.498 | 0.377 ns |  | 1.852*10-3
RMS Electronic Coupling
Reorganization Energy
Marcus Rate
Distance Between Layers
Charge Carrier Hopping
Mobility
Notes: Sources:
https://www.researchgate.net/figure/Schematic-illustration-for-2D-perovskites-3D-perovskites-and-mixed-dimensional_fig1_356789331

## Slide 9: Fluorine as a Structural Stabilizer
 | Average Displacement (Å) |  |  |  |  |  |  | 
 | Pb | I | N | H | C | F | Organic Spacers | Inorganic Crystals
Non-Fluorinated | 0.71 | 0.83 | 1.04 | 1.46 | 0.91 | - | 1.25 | 0.81
Fluorinated | 0.63 | 0.74 | 0.86 | 1.21 | 0.73 | 1.01 | 1.02 | 0.72
Displacement decreases with addition of fluorine atoms
F
Notes: Sources:
https://www.researchgate.net/figure/Schematic-illustration-for-2D-perovskites-3D-perovskites-and-mixed-dimensional_fig1_356789331

## Slide 10: Conclusions
Fluorine substitution enhances the PCE of the 2D perovskite not through coupling effects but through reorganization energy and structural stabilization.
HOMO ~ -2.5 eV
HOMO ~ -2.75
 | Organic Spacers | Inorganic Crystals
BZA | 1.25 | 0.81
F-BZA | 1.02 | 0.72
Notes: Sources:
https://www.researchgate.net/figure/Schematic-illustration-for-2D-perovskites-3D-perovskites-and-mixed-dimensional_fig1_356789331

## Slide 11: Thank you!
Collaborators
Wei Li
Claudio Quarti
David Beljonne
Advisor
Oleg Prezhdo
Notes: Sources:
https://www.researchgate.net/figure/Schematic-illustration-for-2D-perovskites-3D-perovskites-and-mixed-dimensional_fig1_356789331

## Slide 12: Extra Slides

## Slide 13
Notes: SOURCE: https://pubs.acs.org/doi/10.1021/acs.chemmater.2c00146